## Slide 1: E-Tablet Fire Tests: Storage in the aircraft
Systems Meeting
Thomas Maloney, FAA Fire Safety
5-12-2015

## Slide 2: Background
E-tablets are increasing in popularity as supplied personal entertainment device aboard passenger aircraft.
E-Tablets are also used by flight attendants and pilots as electronic flight bags.

## Slide 3: Background
Tests were conducted in a galley cart to assess hazard of bulk-stored tablets. (Report recently published)

## Slide 4: Introduction
E-tablet fire tests were performed in the forward galley of a fully functional 727 to assess the potential fire and explosion hazard of the compartment, toxic gas concentration increase in the cabin and temperature rise in the compartment.

## Slide 5: Test Setup
Aircraft ventilation was on.
Temperature data was collected with a heater T/C, a tablet T/C, a compartment ambient T/C and an IR camera on the outside facing the compartment.
CO, CO2 and O2 gas concentration data was collected in the walkway near the compartment.

## Slide 6: Procedure
A tablet was placed in the compartment and the door was closed.
Thermal runaway was initiated with a heater plate.
A spark igniter was activated to ignite the gasses in test 3 and 4 if they didn’t ignite naturally.

## Slide 7: Test Setup (con’t)
Each of the two tablets was tested once with the igniter and once without it.
 | Spark Igniter | E-Tablet Type 1 | E-Tablet Type 2
Test 1 |  | X | 
Test 2 |  |  | X
Test 3 | X | X | 
Test 4 | X |  | X

## Slide 8: Results

## Slide 9: Results
Chart: Time (minutes)
Increase in CO and CO2 concentrations correspond to thermal runaway events.

## Slide 10: Results (con’t)
 | Max CO (ppm) | Max CO2 (ppm) | Max Compartment Temp (°C)
Test 1 | 97.6 | 128 | 86
Test 2 | 140 | 247.6 | 63.6
Test 3 | 81.3 | 245 | 149
Test 4 | 94.8 | 188 | 112.9
Lower temperatures were observed in Test 1 and Test 2 due to lack of ignition.
Maximum temperature outside the compartment was 81°C observed in test 3.

## Slide 11: Summary
The galley compartment was able to withstand the pressure rise from combustion in these configurations.
Gas concentrations within the cabin remained below the human toxicity limit though a larger number of tablets involved in the fire could prove more dangerous.

## Slide 12: Questions?
Contact
  Thomas Maloney
  Office: 609-485-7542
  Thomas.Maloney@faa.gov