## Slide 1: Lithium Battery Thermal Runaway Initiation Variation
Triennial Conference, Atlantic City
FAA Fire Safety
10/2016

## Slide 2: Background
Lithium Metal cells
  RTCA SC235 is creating a standard for lithium metal batteries aboard aircraft and there was disagreement about different thermal runaway initiation methods.
Lithium Ion cells
  SAE G-27 is creating a packaging standard for shipment of lithium batteries and cells aboard aircraft and a heating rate needs to be specified in the document

## Slide 3: Introduction
Lithium Metal
  There are numerous methods to initiate thermal runaway in a lithium metal cell.
    Overheat
    Overcharge
    Reverse Charge
    Internal short circuit
    Damage
  How does the maximum temperature rise and gas production vary?
  How consistent is the temperature rise and gas production for a specific method?
Lithium Ion
  How does a change in heating rate effect thermal runaway?
    Maximum temperature
    Gas composition

## Slide 4: Thermal Runaway Methods
Overheat – Cell is heated with an external heat source (cartridge or heat strip).
Overcharge – A voltage approximately 1.5* the nominal voltage is applied to the cells with a current limitation of approximately 10C
Reverse Charge – A negative voltage is applied to the cell to cause thermal runaway.

## Slide 5: Test Setup
Tests were carried out in a 21.7L combustion sphere.
Pressure Transducer
Gas collection port for sample bag.
In all tests, air was removed and replaced with 14.7 psia N2 before thermal runaway initiation

## Slide 6: Test Setup
Lithium Metal Cells
  LiSO2
    Overheat
  LiMnO2
    Overheat
    Overcharge
    Reverse charge
  LiFeS2
    Overheat
    Overcharge (if cells are available without PTC)
    Reverse charge (if cells are available without PTC)
  LiCFx
    Overheat
    Overcharge
    Reverse Charge
Lithium Ion Cells
  LiCoO2
    Slowest heating rate (.3 C/min)
    Fastest heating rate (26.7 C/min)
    5 to 10 C/min

## Slide 7: Gas Analysis
Partial pressures were used to determine gas volumes.
GC, NDIR, FID were used for gas concentrations.
  GC:
    Hydrogen
    Methane
    Ethane
    Ethylene/Acetylene
    Propane
    Propylene
    Butane
    Butene
  NDIR
    CO
    CO2
  FID
    THC

## Slide 8: Example Test Setup (Heater Strip)
Heater Strip Capacity: 28 volts, 1.5 amps
Thermocouple
Heater Strip

## Slide 9: Example Test Setup (Overcharge/Reverse Charge)
Thermocouple
Electrical Connection
Electrical Connection
Overcharge/Reverse Charge

## Slide 10: Results LiMnO2 123a
 | Heater | Overcharge | Reverse Charge
Gas Volume (L) | 1.95 | 2.91 | Unable due to PTC
THC (%) | 16.438 | 8.5 | Unable due to PTC
Hydrogen (%) | 27.48 | 26.14 | Unable due to PTC
CO (%) | 24.59 | 15.97 | Unable due to PTC
CO2 (%) | 22.143 | N/A | Unable due to PTC
Max Temp. (C) | 564 | 690 | Unable due to PTC
 | Gas Volume (L) | Max Temp. (C)
Heater Test 1 | 1.95 | 564
Heater Test 2 | 1.95 | 626
Heater Test 3 | 1.83 | 656
Overvoltage test: voltage varied. Initially it was set to 1.5*nominal and maintained for about a day. It was then increased gradually until runaway occurred.

## Slide 11: Results LiCFx A
 | Heater | Overcharge | Reverse Charge
Gas Volume (L) | 1.77 | Unable due to PTC | Unable due to PTC
THC (%) | 26.1 | Unable due to PTC | Unable due to PTC
Hydrogen (%) | 37.9 | Unable due to PTC | Unable due to PTC
CO (%) | 3.6 | Unable due to PTC | Unable due to PTC
CO2 (%) | 2.4 | Unable due to PTC | Unable due to PTC
Max Temp. (C) | 587.8 | Unable due to PTC | Unable due to PTC
 | Gas Volume (L) | Max Temp. (C)
Heater Test 1 | 1.7714 | 587.8
Heater Test 2 | 1.7714 | 660.9
Heater Test 3 | 1.594 | 657.8

## Slide 12: Results LiSO2 D
 | Heater | Overcharge | Reverse Charge
Gas Volume (L) | 6.774 | N/A | N/A
THC (%) | 4.6 | N/A | N/A
Hydrogen (%) | .189 | N/A | N/A
CO (%) | 0 | N/A | N/A
CO2 (%) | .346 | N/A | N/A
Max Temp. (C) | N/A | N/A | N/A
LiSO2 did not show a thermal runaway temperature increase

## Slide 13: Results LiFeS2 AA
 | Heater | Overcharge | Reverse Charge
Gas Volume (L) | 1.0599 | N/A | N/A
THC (%) | 23.82 | N/A | N/A
Hydrogen (%) | 56.4 | N/A | N/A
CO (%) | 6.016 | N/A | N/A
CO2 (%) | 0 | N/A | N/A
Max Temp. (C) | 555.6 | N/A | N/A
Note: Heater temperature needed to reach 445C for runaway to occur

## Slide 14: Results Heating Rate
 | Low Heating rate | 5 to 10 C/min | Fast Heating rate
Heating Rate (C/min) | .315* | 7.3 | 26.74*
Gas Volume (L) | 1.19 | 1.77 | 1.44
THC (%) | 19.6558 | 14.85 | 17.2
Hydrogen (%) | 28.2395 | 27.4455 | 24.33
CO (%) | 6.029 | 10.875 | 8.3271
CO2 (%) | 33.22 | 25.725 | 28.1
Max Temp. (C) | 275.1* | 367.8 | 364.47*
*Result from only one test
Average results (2 tests)

## Slide 15: Results Heating Rate
 | Low Heating rate | 5 to 10 C/min | Fast Heating rate
Gas Volume (L) | .26 | 0 | .066
THC (%) | 5.33 | .15 | .79
Hydrogen (%) | 4.83 | 1.18 | 2.26
CO (%) | 1.07 | .825 | 1.55
CO2 (%) | 5.67 | 3.83 | 1
Standard Deviation

## Slide 16: Results Heating Rate
Chart: Time (seconds)
Typical Test
Largest cause of gas variation
Chart: Time (seconds)
Cell ruptures from pressure
Electrolyte evaporates
More time before runaway
  More evaporation
  Less electrolyte available to react during runaway.
  Less gas volume.

## Slide 17: Summary
Lithium metal
  Consistency in heater strip results.
  1.5*nominal voltage wasn’t sufficient to cause runaway after a day.
  At higher c-rates PTCs interfered with additional overvoltage, reverse charge tests.
Lithium ion
  The lower heating rate resulted in lower temperature increase, less gas volume, less consistency
    A larger amount of electrolyte evaporated from the cell before runaway.
  5 to 10 C/min and higher resulted in higher temperatures and gas volume

## Slide 18: Future Work
MnO2 cells without build-in PTC’s were recently aquired for future tests.

## Slide 19: Questions?
Contact information:
  Thomas.Maloney@faa.gov
  1-609-485-7542