## Slide 1: 8th Triennial International Aircraft Fire and Cabin Safety Research Conference
Development of New Flammability Tests for Magnesium-Alloy Cabin Components
8th Triennial Conference on Aircraft Fire and Cabin Safety Research, Tropicana Hotel Casino, Atlantic City, NJ
Tim Marker, FAA Technical Center
October 24-27, 2016

## Slide 2
Key Activities and Timeline
(2007) IAMFTWG Mag Task Group formed
Discuss Threats
Initial Lab-Scale Testing
Potential Areas of Use
Establish Need for Threat-Based Test
(2006) FAA approached by industry to discuss potential use of magnesium in aircraft
(2007-2008) Initial Phase of Research
(2008-2010) Full-Scale Testing
(2010-Present) Final Phase of Research
Lab-Scale Test Development (oil burner)
Final FAA Policy
Finalize Lab-Scale Test
Lab-Scale Test Into Fire Test Handbook
Develop In-flight Flammability Test

## Slide 3
Magnesium Alloy Use in Commercial Aircraft
Industry Question: Why can’t Magnesium-Alloy be used in the construction of an
aircraft seat frame?
Regulatory Response: Current FAA TSO C-127 “Rotorcraft and Transport Airplane
Seating Systems” makes reference to SAE standard (AS8049), “Performance
Standard for Seats in Civil Rotorcraft, Transport Aircraft and General Aviation”
Para 3.3.3 states, “Magnesium alloys shall not be used.”

## Slide 4
Initial Laboratory-Scale Testing (2007-2008)

## Slide 5
Method: Conduct baseline tests using OEM aluminum-framed triple seats. Tests will simulate a post-crash fire with fuselage rupture, allowing external fire to directly impact the cabin materials.
Then…
Conduct additional tests in an identical fashion using mag-alloy in the construction of the primary seat components. External fuel fire permitted to burn for 5 minutes, then internal fire permitted to burn for 5 additional minutes before applying water.
Outcome: Determine if the use of mag-alloy poses additional hazard during the
10-minute event.
Full-Scale Testing (2008-2010)

## Slide 6
Primary Seat Components
Spreader
Cross Tube
Leg

## Slide 7
Full-Scale Test Apparatus
water applied at end of all tests
(not just magnesium), for similarity

## Slide 8
Full-Scale Testing

## Slide 9
Full-Scale Test Configuration

## Slide 10
Typical Test Result

## Slide 11
Chart: Temperature Comparison Fwd Cabin @ 5 feet

## Slide 13
Incapacitation results very similar for baseline and mag-alloy tests
Noticeable difficulty extinguishing burning mag-alloy during AZ31 test
Slight flashing of burning mag-alloy during water application for WE43 test
slightly better for mag-alloys at forward location
slightly worse for mag-alloys at mid location
More severe fire condition caused more rapid incapacitation during
“all-mag” tests
Full-Scale Testing Summary
Magnesium alloy components had little/no effect on survivability

## Slide 14
http://www.fire.tc.faa.gov/pdf/AR11-13.pdf

## Slide 15
Spring 2007
Spring 2011
Horizontal Bar
Vertical Cone
Various Shapes
Summer 2011
Hollow Cylinder
Horizontal Bar
Spring 2012
Shorter cones
Taller cones
Stepped cones
Rectangular stepped shape
Horizontal cylinders
Rectangular tubing horizontal
Rectangular tubing vertical
I-Webs horizontal
T-Webs horizontal
Inverted cones
Cylindrical tubes horizontal
Cylindrical tubes vertical
Development of a Lab-Scale Test

## Slide 16
Magnesium Alloy Flammability Testing Rig

## Slide 17
Inter-Laboratory Studies (2013-2015)
I
II
III

## Slide 18
https://www.fire.tc.faa.gov/pdf/TC-13-52.pdf

## Slide 19
The Use of Magnesium Alloy in Cabin Areas
Use in 5 primary
seat components
Use in other
cabin components
What is the appropriate method of test?
Oil Burner
Use in other non-primary
seat components
Seatback frame
Crosstubes
Spreaders
Legs
Luggage bar

## Slide 20
Non-Primary Seat Components
tray tables
tray table arms
hardware

## Slide 21
Non-Primary Seat Components
What is the appropriate method of test, since these components were not
represented during full-scale tests?
Consider surface area-to-volume (SAV) ratio…
Higher SAV
Higher Probability of Ignition
Lower SAV
Lower Probability of Ignition
SAV Ratio = 2.2
SAV Ratio = 63.1

## Slide 22
Surface Area-to-Volume (SAV) Ratios of Seat Components
SAV ratio solid component ≤ 20
SAV ratio hollow component ≤ 40

## Slide 23
The Use of Magnesium Alloy in Cabin Areas
Use in 5 primary
seat components
Use in other
cabin components
Accessible
Below seat height
Inaccessible
What is the appropriate method of test?
Oil Burner
Oil Burner
Accessible
Above seat height
Use in other non-primary
seat components
SAV ratio req

## Slide 24
Accessible Components Below Seatback Height

## Slide 25
The Use of Magnesium Alloy in Cabin Areas
Use in 5 primary
seat components
Use in other
cabin components
Accessible
Below seat height
Inaccessible
What is the appropriate method of test?
Oil Burner
Oil Burner
Accessible
Above seat height
Use in other non-primary
seat components
SAV ratio req
Oil Burner
SAV ratio req

## Slide 26
Accessible Components Above Seatback Height

## Slide 27
The Use of Magnesium Alloy in Cabin Areas
Use in 5 primary
seat components
Use in other
cabin components
Accessible
Below seat height
Inaccessible
What is the appropriate method of test?
Oil Burner
Oil Burner
Accessible
Above seat height
Use in other non-primary
seat components
SAV ratio req
Oil Burner
SAV ratio req
Oil Burner
SAV ratio req
?
Ignition/Self
Extinguishment
?
Run full-scale test
?

## Slide 28
Testing of Thin Magnesium Sheet in Radiant Panel
Initial Testing:
3- by 4-inch sample size
3- by 3-inch sample size
3- by 6-inch sample size
Objective: force ignition of sample, and
determine it’s ability to self extinguish
Electrical arc testing

## Slide 29
3- by 6-inch Thin Magnesium Sample
Initial piloted ignition
Burn

## Slide 30
3- by 6-inch Thin Magnesium Sample

## Slide 34
Results of 3- by 6-inch Magnesium Sample Testing
When using 3- by 6-inch sample size, good separation between good and poor alloys
Time of ignition may not be important, provided the sample demonstrates ability to
self-extinguish
Increased sample length allows sample the opportunity to self extinguish
Weight loss consistent per alloy, between 5 and 30%
Weight loss more accurate assessment of amount of burning
Difficult to ignite 0.050-inch sample thickness; 0.025-inch thickness more appropriate
Ignition often occurs as pilot flame is removed

## Slide 35
Wrap-Up, Conclusions, Future Work
Discuss use of magnesium alloy components located in accessible areas that are
situated higher than seat back height. Is there a need to conduct full-scale tests?
Finalize test parameters and pass/fail criteria for magnesium alloy components
located in inaccessible areas:
Radiant Panel Apparatus, 3- by 6-inch sample size, 0.025-inch thickness
No ignition before 60 seconds (proposed)
Maximum weight loss of 30% (proposed)
Investigate use of sample holder to prevent thin test samples from curling or lifting.

## Slide 36
Questions?