## Slide 1: AIRBUS Project FaBLE
Development and validation of a foam block equivalent
FAA-IAMFTWG June 2015 Bremen
Thomas Vielhaben
ESCMB2

## Slide 2: Content
What is FaBLE?
Foam Block Properties
Project Requirements
Project Implementation
Project Validation
  Heatflux / Temperature
  Coupon test
Conclusion

## Slide 3: What is FaBLE?
FaBLE is an equivalent to the FAA-TC hidden area fire source (Foam Block Equivalent)
FaBLE reproducably reflects the foam block properties
FaBLE is simlpe in use
?

## Slide 4: Foam Block Properties
Blackening flame
10 ml heptane
ca. 1200 kJ
4 in
4 in
9 in
(102 mm x 102 mm x 229 mm)
4 in
Heatflux ca. 7.25 W/cm²
About 1150 °F (620 °C)

## Slide 5: Foam Block Properties
  0 – 60 s: primary phase, high heatflux, most of damage
  >60 s: secondary phase, low heatflux, few additional damage
4 in
4 in
9 in
(102 mm x 102 mm x 229 mm)
Primary
phase
Secondary
phase
4 in
Heatflux ca. 7.25 W/cm²
About 1150 °F (620 °C)

## Slide 6: Requirements for FaBLE
Operation/construction
Easy handling
Safe concept
Simple construction (standard parts)
No aging effects
Same geometry as foam block
Equal maximum heatflux and comparable heatflux evolution
Equal maximum temperature and comparable temperature evolution
Similar calorific value
FaBLE
Properties

## Slide 7: Implementation: Setup
Propane
Laptop
ARDUINO controller
Gas burner
MFC
Heat mesh
booster
0-10 l/min
0 or 10 l/min

## Slide 8: Implementation: Setup
Propane
Laptop
ARDUINO controller
Gas burner
MFC
Heat mesh
Valve sequence to create foam block heat release profile
 Calculated from 11 foam block tests

## Slide 9: Implementation: Setup
Propane
Laptop
ARDUINO controller
Gas burner
MFC
Heat mesh
Arduino & Shield
Valve –Amp..
PS.
Booster.
MFC.

## Slide 10: Implementation: Human interface

## Slide 11: Validation: Comparison of heatflux
Foam block
FaBLE

4 in
4 in
9 in
(102 mm x 102 mm x 229 mm)
4 in
Gordon gauge calorimeter type K thermocouple
Equal max. heatflux
Equal temperature profile

## Slide 12: Validation: Coupon test
4 in
5 in
temperature
24 in
FaBLE (or foam block)
Specimen (width 13 in)
angle of 45 degrees

## Slide 13: Validation: Coupon test
4 in
5 in
FaBLE (or foam block)

Equal max. temperature and temperature plot
Low temperature deviation in the secondary phase due to heat mesh radiation
temperature
24 in
Specimen (width 13 in)

## Slide 14: Validation: Coupon test

Foam Block
FaBLE
PE cellular material 25mm

## Slide 15: Validation: Coupon test

Foam Block
FaBLE
Foam Block
FaBLE
FaBLE
Foam Block
Foam Block
FaBLE
C-EP-53% three layers
PC 3mm
to PHG-50% - test side
to PHG-50% - test side

## Slide 16: Conclusion
All specified requirements will be fulfiled
FaBLE is a reproducible fire source and represents foam block properties
FaBLE is a low cost device, made from world wide available standard parts
FaBLE is an equivalent to the hidden area fire source
For further validation we will send one of our first series model to FAA tech-center

## Slide 17
© Airbus Operations GmbH. All rights reserved. Confidential and proprietary document. This document and all information contained herein is the sole property of Airbus Operations GmbH. No intellectual property rights are granted by the delivery of this document or the disclosure of its content. This document shall not be reproduced or disclosed to a third party without the express written consent of Airbus Operations GmbH. This document and its content shall not be used for any purpose other than that for which it is supplied. The statements made herein do not constitute an offer. They are based on the mentioned assumptions and are expressed in good faith. Where the supporting grounds for these statements are not shown, Airbus Operations GmbH will be pleased to explain the basis thereof. AIRBUS, its logo, A300, A310, A318, A319, A320, A321, A330, A340, A350, A380, A400M are registered trademarks.