## Slide 1: Inaccessible Area Fire Tests on Composite Structure - Update

## Slide 2: CFRP Aircraft Structures
Carbon fiber composites are being used more frequently in aerospace applications
  Increased strength
  Lower density
  Better corrosion resistance
New designs of commercial transport airplanes include primary and secondary structure constructed from carbon fiber composites
14CFR 25.853 specifies requirements for flame resistance of cabin interior materials (panels, seat cushions, fabrics, etc.)
Current FAR’s do not require flammability testing for fuselage skins or structures, as traditional designs are inherently non-flammable
  Special Conditions for certification of fire resistance of composite fuselage
  Must demonstrate level of safety equivalent to or better than traditional constructions
To continue with the FAA’s efforts to enhance in-flight fire safety, materials in inaccessible areas of the cabin should meet a flammability test based on the “block of foam” fire source

## Slide 3: Initial CFRP Flammability Testing
Stringer
Shear Tie
Frame
Flaming Block of Foam

## Slide 4: ET-AOP 787 Fire, London Heathrow, July 2013

## Slide 5
Outlet Temp [°F] | Inlet Temp [°F] | ΔT [°F] | Flowrate [mL/min] | Flowrate [GPH] | Flowrate [lb/hr] | Q [BTU/hr] | Q'‘ [BTU/ft2s] | Q'‘ [W/m2]
125 | 116 | 9 | 2070.00 | 32.81 | 272.32 | 2477.25 | 0.15 | 1666.53
Ti=116°F
To=125°F
Flowrate=272.32 lb/hr
Heater Power Input = 843 Watts=
Heat Transfer Calculation Error =
Power Supply
To Blanket Heater

## Slide 6
In flight conditions:
  M=0.85
  Velocity
  Altitude=40,000’=12,192m
    Density
    Dynamic Viscosity1
    Temperature
    Pressure
Reynolds Number
  Characteristic Length (fuselage length)
  Thermal Conductivity1
  Dynamic Viscosity1
  Thermal Conductivity1
1 Viscosity and Thermal Conductivity of Dry Air in the Gaseous Phase K. Kadoya, N. Matsunaga, A. Nagashima, J. Phys. Chem. Ref. Data, Vol. 14, No. 4, 1985

## Slide 7
Flat Plate in Parallel Flow with Unheated Starting Length
Uniform surface heat flux, turbulent flow, unheated starting length
  , 0.6≲Pr ≲60
Fire
Aircraft Skin

## Slide 8
At an ambient air temperature of -70°F (216K)
Need to calculate outside surface temperature
~500°F (533K) : observed during CFRP burn tests with FLIR
70°F (294K) : inside cabin temperature
For Ts of 500°F (533K), q’’=18,145 W/m2
For Ts of 70°F (294K), q’’=4,464 W/m2
Heat Transfer Rig Only Reaches q’’=1,666 W/m2
With current configuration
Corresponds to a Ts of 245K=-18.67°F

## Slide 10
6 ¾”
2 ½”
Gas Measurement
Channel Dimensions
Simulated ELT
Ignition Source
Insulation Attached
To Test Fixture

## Slide 14: Heat Transfer Calculation
Energy required for water heating
    Q is heat, BTU
    m is mass of water heated, lb.
    cp is heat capacity of water,
    is temperature difference,
Heat Flux
  Q’’ is heat flux,
  A is area, ft2
  t is time, sec
Ti
To

## Slide 15
Estimated in-flight cooling:
For Ts of 500°F (533K), q’’ = 18,145 W/m2
For Ts of 70°F (294K), q’’ = 4,464 W/m2
Heat Transfer Rate Calculated From Cooling Water ΔT
Measured Heat Transfer Max = 1,617 W/m2
Below estimated in-flight range of
4,464 to 18,145 W/m2

## Slide 16: Next Test
During previous test, the most damage was found on structure that was not in direct contact with outboard cooled surface
A second test will be performed with additional structure, including stringers, frames, and shear ties, that are not in contact with the outboard surface